BSD-68301 Medium-speed Cylindrical Piston Engine Oil Additive Package

Product Performance

This product is compounded with high-temperature detergents, ashless dispersants, antioxidant and anticorrosion agents, ashless multi-effect high-temperature antioxidants and rust inhibitors. It has good detergency, base number retention properties, rapid acid neutralization ability and water-separation performance. It effectively protects the performance of the engine. After long-term use, the engine has minimal wear and tear and no obvious signs of rust. It also can keep the interior of the engine clean.

Recommended Dosage

30TBN: 15.0%;  40TBN: 19.0%;  50TBN: 22.0%

Technical Parameter

| Item | Quality Index | Test Method |
| --- | --- | --- |
| Kinematic Viscosity(100℃), mm²/s | Measured Value | GB/T265 |
| Flash Point (Open Cup), ℃ | ≥180 | GB/T3536 |
| Calcium Content, m/m % | ≥6.0 | SH/T0270 |
| Zinc Content, m/m % | ≥0.75 | SH/T0226 |
| Nitrogen Content, m/m % | ≥0.25 | SH/T0224 |
| Total Base Number, mg KOH/g | ≥170 | SH/T0251 |