BSD-68602  SM/SN Grade/A3/B4

Gasoline Engine Oil Compound Additive

Product Performance

This product is formulated with high-grade detergents, ashless dispersants, long-chain ZDDP anioxidant and anticorrosion agent, high-temperature antioxidants, friction modifiers and metal deactivators. It is an energy-saving gasoline engine oil compound additive specially formulated for the GF series of products that comply with the ILSAC international standards and high-grade oils of API SM and SN. It has outstanding antiwear, friction-reducing, restorative performance and anti-scuffing ability. It can extend the service life of components and reduce organic gas carbon emission. It has excellent detergent-dispersancy, fuel economy and a relatively long oil change interval. In API Group II, III and IV base oils, by combining with the corresponding viscosity index improver, various grades of ACEA Group A3/B4 oils can be blended.

Scope of Application and Recommended Dosage

It is applicable to API Group I, II, III and IV base oils and can meet the high grade energy-saving and environmentally friendly gasoline engine oil in both the European ILSAC , ACEA and American API standards.

Recommended dosage: SM: 7.5%; SN/CF-5: 7.8%; ACEA A3B4: 10.5% +0.25%BSD-WT355

Technical Parameter

| Item | Quality Index | Test Method |
| --- | --- | --- |
| Kinematic Viscosity(100℃), mm2/s | Measured Value | GB/T265 |
| Flash Point (Open Cup), ℃ | ≥190 | GB/T3536 |
| Total Base Number, mg KOH/g | ≥86 | SH/T0251 |
| Sulfur Content, m/m % | ≥2.2 | SH/T0303 |
| Calcium Content, m/m % | ≥2.6 | SH/T0270 |
| Phosphorus Content, m/m % | ≥0.9 | SH/T0296 |
| Zinc Content, m/m % | ≥1.0 | SH/T0226 |
| Molybdenum Content, m/m % | ≥0.06 | ASTM D5185 |
| Magnesium Content，m/m % | ≥0.01 | ASTM D5185 |