BSD-68701 CF-4/CH-4 Grade Diesel Engine Oil

Compound Additive

Product Performance

This product is formulated with metal detergents, ashless dispersants, antioxidation and anticorrosion agents and metal deactivators, etc. It has excellent thermal oxidation stability, antiwear performance, friction-reducing properties, anticorrosion performance, seal adaptability, as well as energy-saving and emission-reduction effects. It pays more attention to the problems of turbocharged diesel engines such as high soot content, high acid value, heavy load and high temperature, which are likely to cause problems like excessive sulfated ash in the cylinders, piston ring corrosion, cylinder liner wear, high oil temperature in the crankcase and rapid oxidation.

Scope of Application and Recommended Dosage

It is suitable for formulating various vehicle diesel engine oils with API Group I, II, III and IV base oils.

Recommended dosage: CF-4: 6.0%; CH-4: 7.6%

Technical Parameter

| Item | Quality Index | Test Method |
| --- | --- | --- |
| Kinematic Viscosity(100℃), mm2/s | Measured Value | GB/T265 |
| Flash Point (Open Cup), ℃ | ≥185 | GB/T3536 |
| Total Base Number, mg KOH/g | ≥120 | SH/T0251 |
| Calcium Content, m/m % | ≥4.2 | SH/T0270 |
| Zinc Content, m/m % | ≥1.3 | SH/T0226 |
| Nitrogen Content, m/m % | ≥0.65 | SH/T0224 |
| Phosphorus Content, m/m % | ≥1.1 | SH/T0296 |