BSD-68702  CI-4 Grade Diesel Engine Oil Additive Packadge

Product Performance

This product is formulated with high-efficiency detergent, high-molecular ashless dispersant, borated ashless dispersant, friction- reducing agent, ZDDP antioxidation and antiwear additive, as well as high-temperature antioxidation additive. It has excellent thermal oxidation stability, antiwear performance, friction-reducing properties, anticorrosion performance, seal adaptability, energy-saving and emission-reduction effects, as well as high-temperature detergency, low-temperature dispersibility, alkali retention performance and adaptability to various base oils.

Scope of Application and Recommended Dosage

It is suitable for using API Group I, II, III and IV base oils to formulate various diesel engine oils for vehicles that meet the ACEA and API standards.

Recommended dosage: CH-4: 7.5%; CI-4: 8.5%

Technical Parameter

| Item | Quality Index | Test Method |
| --- | --- | --- |
| Kinematic Viscosity(100℃), mm2/s | Measured Value | GB/T265 |
| Flash Point (Open Cup), ℃ | ≥190 | GB/T3536 |
| Total Base Number, mg KOH/g | ≥105 | SH/T0251 |
| Phosphorus Content, m/m % | ≥0.9 | SH/T0296 |
| Calcium Content, m/m % | ≥3.4 | SH/T0270 |
| Nitrogen Content, m/m % | ≥0.7 | SH/T0224 |
| Zinc Content, m/m % | ≥1.1 | SH/T0226 |